## Slide 1: Quasielastic Neutron Scattering Studies of Hybrid Perovskites
M.K. Crawford and N. Herron (DuPont)
M. Tyagi (NIST)
N. Jalarvo (ORNL)
November 25, 2014

## Slide 2: Quasielastic and Inelastic Neutron Scattering
Energy Transfer

## Slide 3: Elastic fixed window scans
Measure intensity of elastic scattering vs T
Intensity of elastic scattering decreases as intensity transforms to quasielastic scattering
  QENS reflects the presence of dynamical processes that exceed the energy resolution of the NIST back-scattering spectrometer
    Resolution = 0.8 meV ~ 0.006 cm-1
    In time domain, this corresponds to processes that occur on the 10-9-10-12 sec timescale

## Slide 4: Mean Square Displacement: MAPbI3
Main Features
  Cubic-tetragonal transition near 330 K does not affect MA cation dynamics
    Pm3m  I4/mcm
  First-order structural phase transition (orthorhombic  tetragonal) at Tc = 160 K
  Dynamics first appear near 60 K
    Methyl or MA rotations?
  Quasielastic scans were then collected at various temperatures based upon this result

## Slide 5: QENS vs Dielectric Constant
Cubic-tetragonal transition at 330 K does not affect MA cation dynamics or dielectric properties
  Free rotation of MA cation
Strong drop in MSD and dielectric constant at tetragonal-orthorhombic phase transition
  MA reorientations become restricted below Tc
  Low T dynamics associated with rotations of methyls or MA ions around C-N axis (no orientation of dipole moments shown by dielectric constant)
  Similar hysteresis

## Slide 6: Mean Square Displacement: MAPbBr3
Main features
  Cubic-tetragonal transition at 236 K does not appear (as for iodide)
  Pm3m  I4/mcm
  Two structural transitions near 150 K
    Tetragonal 1  tetragonal 2
    Tetragonal 2  orthorhombic
  Low temperature dynamics first appear near 30 K
    60 K in iodide!

## Slide 7: Mean Square Displacement: MAPbBr0.75I2.25
Main features
  Smoothly increasing MSD
  No sign of structural phase transition(s)!
    At least no first-order (discontinuous) transitions
  Sample is at APS for x-ray diffraction vs T

## Slide 8: Mean Square Displacement: MAPbCl3
Main features
  Cubic-tetragonal 2 transition
    Dielectric constant changes here
    Pm3m  P4/mmm
  Two first-order structural phase transitions
  Two step dynamical transition starting at 30 K

## Slide 9: Quantum Mechanical Tunneling
Tunnel transitions appear at T = 4 K
  Only observed in MAPbCl3
  Just barely observable with HFBS spectrometer resolution of 0.8 meV
MA cation rotations?
Methyl rotations?
Impurity phase?
  Check synchrotron XRD
If due to MAPbCl3, provides a measure of rotational barrier height
Q = 1.32 Å-1

## Slide 10: Next steps
Complete data analysis for activation energies of dynamics below T = 100 K
See is bromoiodide has any structural transitions
  Suppressed by halogen disorder?
Next two weeks
  Continue QENS and INS measurements at ORNL
  Neutron diffraction determination of structures of fully deuterated samples
    Especially MAPbI3
  PDF analysis of disordered structures using POWGEN data?